Ntgrate Wall covering (wall paper)

**Technical data sheet**

The synthetic wall covering »**Ntgrate**» is a flat woven synthetic quality. In the weaving process, the TOPGRATE® technology only uses, glass-fiber reinforced, PVC yarns of which **an adhesion between the core and the skin > 20 N.** The fabric, with **a warp density of 12 threads/cm** and a weft density of an average of 9 threads/cm, is **stabilized in a heat set process.** The ntgrate wall covering is available in a width of 100 mm . The ntgrate® wallpaper is available in 14 colors and 2 designs. Every reference is also available as flooring.

|  |  |  |  |
| --- | --- | --- | --- |
| Thickness :  Width : | ca 1,5 mm  100 mm |  |  |
| Total Weight : | ca 800 gr/m² |  |  |
| Material composition :  Backing :  Yarn density : | Fiberglass 17%  PVC 73%  10%  Warp: 18 – Weft 14 |  |  |
|  |  |  |  |
| Resistance to fire :  EN ISO 11925-2 : EN ISO 13823 : | Bs3d0 |  |  |
|  |  |  |  |